Consolideck® Concrete Floor Restorer Cleaning Specification

Specifier Note: The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information.

Specifier Note: Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use manufacturer’s application instructions. Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note: Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer: PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046. Phone: (800) 255-4255; Fax: (785) 830-9797. E-mail: CustomerCare@prosoco.com

# Product Description

Consolideck® Concrete Floor Restorer is an effective blend of purified acids, oil and grease solvents, floor polish removers and wetting agents to remove a wide variety of common stains and soiling from concrete floors. Once cleaned and dry, floors are ready for repairs, hardening and densifying, and any other treatment aimed at improving appearance, performance and service-life. Concrete Floor Restorer will not affect concrete color. It will remove most old floor waxes, skid marks, rust and other metallic stains, dirt, atmospheric soiling and more.

Consolideck® Concrete Floor Restorer is compatible with all Consolideck® protective treatments, hardeners-densifiers, as well as color coats and stains.

Typical Technical Data

FORM: pale, yellow liquid

SPECIFIC GRAVITY: 1.12

pH Concentrate: 0.20

pH at 1 to 3 dilution: 0.30

pH at 1 to 6 dilution: 0.56

WEIGHT/GALLON: 9.39 pounds

TOTAL SOLIDS: not applicable

VOC CONTENT: not applicable

ACTIVE CONTENT: not applicable

FREEZE POINT: less than 12 degrees F (less than -11 degrees C)

FLASH POINT: greater than 212 degrees F (greater than 100 degrees C)

Limitations

- Acidic contents may damage polished concrete, some non concrete and acid-sensitive surfaces.

- May damage previously color-stained surfaces.

Specifier Note: Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for application instructions.

SPECIFIER NOTE: Multiple applications may etch acid-sensitive surfaces.

Dilution

Test for proper dilution beginning with 1 part cleaner to 6 parts fresh water. Do not exceed 1 part cleaner to 3 parts fresh water. Use the mildest dilution that produces effective results. Always pour water into empty bucket first, then carefully add concentrate. Refer to test panel results for recommended dilution for intended use.

1. Apply cleaner evenly to a dry surface with an acid-resistant mop, applicator or low-pressure spray.

2. Let the cleaning solution dwell on the surface 3-5 minutes or until the stains dissolve. If treated surfaces are left unattended, keep people away from the cleaner. Scrubbing with an acid-resistant brush improves results.

3. Rinse the cleaned area thoroughly with fresh water to get all residues off the surface.

SPECIFIER NOTE: The best combination of rinsing pressure and water volume is provided by masonry washing equipment generating 400 to 1000 psi with a water flow rate of 6 to 8 gallons per minute delivered through a 15 to 45 degree fan spray tip.

SPECIFIER NOTE: Rinsing equipment should be adjustable to reduce water flow rate and rinsing pressure as required for controlled cleaning of more sensitive surfaces. See also “Equipment” section of the Product Data Sheet.

SPECIFIER NOTE: If pressure-rinsing equipment is not available, brush the surface while rinsing with plenty of clean water.

Cleanup

Clean tools and equipment using fresh water.