Consolideck® PreKlean Cleaning Specification

Specifier Note: The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information

Specifier Note: Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use manufacturer’s application instructions. Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note: Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer: PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046. Phone: (800) 255-4255; Fax: (785) 830-9797. E-mail: CustomerCare@prosoco.com

# Product Description

Consolideck® PreKlean is a concentrated cleaner to remove laitance and residual surface salts often associated with blanket curing on newly installed concrete floors for better penetration, bond and effectiveness of hardener/densifiers and other flooring treatments. Consolideck® PreKlean is designed for use immediately curing blankets are removed, or within 3-7 days of installation.

Typical Technical Data

FORM: 	clear liquid

SPECIFIC GRAVITY: 1.29

pH: 4.8

WEIGHT/GALLON: 10.83 pounds

ACTIVE CONTENT: not applicable

TOTAL SOLIDS: not applicable

VOC CONTENT: 0 percent

FLASH POINT: greater than 200 degrees Fahrenheit (greater than 93 degrees Celsius) ASTM D 3278

FREEZE POINT: not applicable

SHELF LIFE: 2 years in unopened, factory-sealed container

Specifier Note: Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Consolideck® PreKlean. Refer to the Product Data Sheet for additional information about application.

Dilution

Dilute one part cleaner concentrate with four parts clean, fresh water. Mix well. Always pour cold water into an empty bucket first, then carefully add cleaner.

When applying with an auto scrubber, add water to tank before adding product.

Application Instructions

Auto-Scrubber

- After removing curing blankets, scrub and vacuum area with clean water.

- Apply PreKlean while scrubbing with squeegee up. Limit application of PreKlean to an area that can be cleaned and scrubbed within 10-15 minutes.

- Scrub while removing PreKlean from the floor with vacuuming.

- Rinse with clean water.

SPECIFIER NOTE: Do not allow surface salts to dry on the surface as blankets are being removed.

Mop or Spray Application

- After removing curing blankets, rinse area with clean water.

- Apply diluted PreKlean with a clean mop or sprayer.

- Let cleaner dwell for 15 minutes.

- Scrub with a deck brush or stiff bristle broom.

- Mop up spent cleaner.

- Rinse with clean water and mop.

Cleanup

Clean tools and equipment with soap and water.