# PROSOCO® Cure & Seal Remover Cleaning Specification

Specifier Note: The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information.

Specifier Note: Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use manufacturer’s application instructions. Let the test panel dry 3 to 7 days before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note: Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046. Phone: (800) 255-4255; Fax: (785) 830-9797. E-mail: CustomerCare@prosoco.com

# Product Description

PROSOCO® Cure & Seal Remover is a water-rinsable cleaner designed to remove the toughest, high-solids cure and seals from horizontal concrete in order to prepare the concrete floors for hardening and densifying. Cure & Seal Remover effectively removes old coatings that can block treatments from penetrating or clog up the heads on grinding and polishing equipment.

# Typical Technical Data

FORM: clear liquid, sweet almond odor

SPECIFIC GRAVITY: 1.04

pH: not applicable

WEIGHT/GALLON: 8.60 pounds

ACTIVE CONTENT: not applicable

TOTAL SOLIDS: not applicable

FLASH POINT: 198 degrees F (92 degrees C) ASTM D 3278

FREEZE POINT: not applicable

SHELF LIFE: 2 years in unopened, factory-sealed container

VOC CONTENT: 30 percent maximum. PROSOCO® Cure & Seal Remover is compliant with all national, state and district VOC regulations.

# Limitations:

- Surfaces are slippery during application. Use appropriate caution.

- Product efficiency is reduced in cold temperatures.

- Product may damage synthetic or reflective glass. Always protect.

Specifier Note: Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Cure & Seal Remover.

Dilution: Apply as packaged. Do not dilute or alter. Use in concentrate.

Coverage: Coverage rates vary based on concrete porosity and texture. Anticipated coverage rate is 300-500 square feet per gallon of cleaner.

# Application Instructions

- Apply product with low-pressure spray.

- Allow to dwell for 5-10 minutes.

- Scrub with a stiff bristle brush or a mechanical scrub machine.

- Take up as much spent cleaner and dissolved coating as possible.

- Rinse or mop the floor with fresh water if needed.

Cleanup: Clean tools and equipment with fresh water.