PROSOCO R-Guard® SureSpan Adhesive Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products distributed and/or manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and Material Safety Data Sheet for additional recommendations and for safety information

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Mock-Ups

Apply to field-constructed mock-up assemblies. Use the manufacturer’s application instructions. Keep mock-ups available for inspection throughout the project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

PROSOCO R-Guard® SureSpan Adhesive is designed to adhere and seal SureSpan EX®, as part of a building-wide R-Guard® air barrier system or to complement conventional waterproofing or air barrier components.

SureSpan Adhesive is a gun-grade adhesive that combines the best of silicone and polyurethane properties. The single-component, Silyl-Terminated-Polymer (STP) is easy to gun, spread and tool. SureSpan Adhesive is suitable for all climates, bonds directly to damp or dry surfaces, and cures under a variety of weather conditions.

# TYPICAL TECHNICAL DATA

FORM: viscous paste with mild odor, gray color

SPECIFIC GRAVITY: 1.48 to 1.58

pH: Not applicable

WEIGHT/GALLON: 12.7 pounds

TOTAL SOLIDS: 99 percent

FLASH POINT: No data

FREEZE POINT: No data

SHELF LIFE: 1 year in unopened, factory-sealed container

VOC: 30 grams per Liter, maximum. Complies with all known national, state and district AIM VOC regulations.

# Limitations

- Not for use as a liquid flashing membrane. Use R-Guard® FastFlash®.

- Not for use in place of appropriate through-wall flashing. See R-Guard® SS ThruWall product literature.

- Not for use installing R-Guard® SS ThruWall.

- Not for use below grade or in locations which are continuously immersed in water.

- Not for use onto asphalt or under specific pressure sensitive adhesive.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Installation

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for R-Guard SureSpan Adhesive.  Refer to the Product Data Sheet for additional information about application.

Use R-Guard SureSpan Adhesive as packaged. Do not dilute or alter. No mixing is required.

Application Instructions: Adhering SureSpan EX

- Apply a bead of SureSpan Adhesive in a straight line near the outside edges of the area to be covered by SureSpan EX®. The bead should be approximately 1/8 to 1/4 inch in diameter, depending on the uniformity of the substrate. Allow enough space for the SureSpan Adhesive to squeeze out to the edge of the SureSpan EX® and then stop. Nonporous surfaces such as glass or aluminum require less sealant; porous substrates such as brick or stone require more.

SPECIFIER NOTE: If installed over a protrusion, such as a fastener, apply a small amount of SureSpan Adhesive on the protrusion to eliminate chaffing during movement.

- Unroll the appropriate length of SureSpan EX® and place it over the joint to be sealed. Within 2–3 minutes, embed SureSpan EX® into the still-wet SureSpan Adhesive. Use a wooden roller or flat piece of wood to press the extrusion firmly into place and ensure full and continuous contact between the SureSpan EX®, SureSpan Adhesive and the substrate.

- Clean or tool any excess SureSpan Adhesive from the edges of the extrusion and substrate. Trim ends and terminate with a bead of SureSpan Adhesive.

SPECIFIER NOTE: Always apply horizontal joints before vertical joints. At intersections overlap the vertical SureSpan EX® over the horizontal and ensure a proper seal by applying sufficient SureSpan Adhesive.

# Curing and Drying

At 70°F (21°C) and 50% relative humidity, product skins within 60 minutes, is transfer free within 4 hours and fully cures in 7 days. Paintable with most paints after 24 hours.

SPECIFIER NOTE: R-Guard SureSpan Adhesive is moisture curing. Low temperatures and low relative humidity slow dry time. High temperatures and high humidity accelerate drying.

# Cleanup

Clean tools and equipment with mineral spirits or similar solvent immediately after use. Follow all safety precautions. Remove cured SureSpan Adhesive mechanically using a sharp-edged tool.