PROSOCO R-Guard® SureSpan EX® Transition Membrane Specification
Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information 

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.  

Mock-Ups:
Apply fluid applied air barrier system to field-constructed mock-up assemblies illustrating material interfaces and seals. Use the manufacturer’s application instructions. Keep mock-ups available for inspection throughout the project. 

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.  

Distributor:  PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

Product Description

PROSOCO R-Guard® SureSpan EX® is a flexible, durable silicone material designed to help create flexible and durable transitions between various types of air and water barriers and the curtainwall, storefront, or window being installed. SureSpan EX® provides a continuous bridge between the window and/or curtainwall openings and the adjacent air and vapor barrier materials. SureSpan EX® is designed for high movement, dynamic joints which are too large to be spanned by R-Guard Joint & Seam Filler or R-Guard FastFlash®. SureSpan EX® absorbs thermal movement and wind-loading stresses. The system spans and seals across irregular window geometries. SureSpan EX® is fully compatible with most window sealants and glazing materials. 

R-Guard SureSpan EX® is an extruded, low modulus, elastomeric, pre-cured sealant that is bonded to substrates with R-Guard FastFlash®. SureSpan EX® is supplied in a translucent caution yellow to simplify inspection and quality control.  
TYPICAL TECHNICAL DATA

FORM: cured silicone rubber, odorless
SPECIFIC GRAVITY: 1.20 at 25 C
VOC CONTENT: not regulated
SHELF LIFE: not applicable
Limitations 

· Not for use below grade.  
· Not for use in permanently exposed conditions.
· Not intended for use as load-bearing, through-wall flashing. 
Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.  

SPECIFIER NOTE: Prepare all joints, seams cracks, fastener penetrations and rough openings prior to application of the primary air barrier. See appropriate product data sheets and R-Guard Installation Guidelines for more information.

Installation
Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for PROSOCO R-Guard® SureSpan EX®. Refer to the Product Data Sheet for additional information about application.  

Application 

1. Apply a bead of R-Guard FastFlash® in a straight line near the outside edges of the area to be covered by SureSpan EX®. The beads should be approximately 1/8 to 1/4 inch in diameter, depending on the uniformity of the substrate. Allow enough space for the FastFlash® to squeeze out to the edge of the SureSpan EX® and then stop. Non porous surfaces such as glass or aluminum require less sealant, porous substrates such as brick or stone require more.

SPECIFIER NOTE:  If installed over a protrusion, such as a fastener, apply a small amount of sealant on the protrusion to eliminate chaffing during movement.

2. Unroll the appropriate length of SureSpan EX® and place it over the joint to be sealed. Within 2–3 minutes, embed SureSpan EX® into the still wet FastFlash®. Use a flat piece of wood or roller to press the extrusion firmly into place to ensure full and continuous contact between the SureSpan EX®, FastFlash® and the substrate. 
3. Clean or tool any excess FastFlash® from the edges of the extrusion and substrate. Trim ends and terminate with a bead of FastFlash®. At intersections simply overlap the vertical SureSpan EX® over the horizontal and ensure a proper seal by applying sufficient FastFlash®.
SPECIFIER NOTE:  Always apply horizontal joints before vertical joints. 
Cleanup

Carefully remove any masking tape and excess FastFlash® before it cures. Remove any additional FastFlash® from adjacent surfaces or from the face of the SureSpan EX® using isopropyl alcohol, mineral spirits or similar solvent. 
