Sure Klean® Strippable Masking  Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and MSDS for additional recommendations and for safety information

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use the manufacturer’s application instructions. Let test area dry thoroughly before inspection. Keep test panels available for comparison throughout the cleaning project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

Manufacturer:  PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® Strippable Masking (White) is a white temporary coating material for protecting glass, unpainted metal, and polished stone from masonry cleaners being used nearby. It is an easily applied liquid that dries to form a temporary coating, protecting surfaces from contact with masonry cleaning solutions. After cleaning is complete, Strippable Masking is easily removed.

Technical Data

FORM: Viscous, white liquid

TOTAL SOLIDS: 30%

SPECIFIC GRAVITY: 1.04

pH: 9.9

WT./GAL.: 8.65 lbs.

FLASH POINT: 444 degrees F (229 degrees C) ASTM D 3278

FREEZE POINT: 32 degrees F (0 degrees C)

VOC CONTENT: Complies with all known national, state and district AIM VOC regulations.

### Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.  `

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Strippable Masking (White).  Refer to the Product Data Sheet for additional information about application of Strippable Masking.

1. Thoroughly stir contents before applying. Apply one heavy coat or two light coats until surfaces are uniformly white, with no dark areas. There should be no pinholes that allow corrosive materials to get behind film.

2. Let treated surfaces dry at least one hour before exposing to acidic washing systems, water pressure or other activity. Typical drying time is 1 hour.

Note: Avoid driect contact with high-pressure rinsing equipment until cleaning operations are complete.

Removal

Leaving Strippable Masking on the surface longer than specified may make removal more difficult. Dry brushing with agitation or high-pressure rinsing may facilitate removal Strippable Masking.

When used outdoors or indoors and exposed to sunlight, remove Strippable Masking within 3 weeks of application.

When used indoors and not exposed to sunlight, remove the film within 8 weeks.

When removing from metal surfaces, start at a corner and peel off. Properly applied coatings come off in large sections.