Sure Klean® Weather Seal Blok-Guard® & Graffiti Control Ultra 15 Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and Safety Data Sheet for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use the manufacturer’s application instructions. Let test area protective treatment cure before inspection. Keep test panels available for comparison throughout the protective treatment project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® Weather Seal Blok-Guard® & Graffiti Control Ultra 15 is a high performance, clear, solvent-based silicone elastomer formulated to weatherproof concrete block and other porous masonry materials and protect treated surfaces from repeated graffiti attacks with little to no change to the natural appearance.

Easily applied with low-pressure spray, brush or roller, Blok-Guard® & Graffiti Control Ultra 15 penetrates and fills pores to prevent water penetration through exterior walls exposed to normal weathering. Graffiti removal is fast and easy using Defacer Eraser® Graffiti Remover.

# Typical Technical Data

FORM: Clear liquid, petroleum odor

SPECIFIC GRAVITY: 1.28

pH: not applicable

WEIGHT/GALLON: 10.62 pounds

ACTIVE CONTENT: 15 percent

TOTAL SOLIDS: 15 percent ASTM D2369

VOC CONTENT: less than 100 grams per Liter

FLASH POINT: 100 degrees F (38 degrees C) ASTM D3278

FREEZE POINT: less than -22 degrees F (less than -30 degrees C)

SHELF LIFE: 1 year in tightly sealed, unopened container

# Limitations

- May darken or enhance the natural color of some surfaces. Always test to ensure desired results.

- Not suitable for extremely dense or polished surfaces.

- Not suitable for asphaltic or painted surfaces.

- Not recommended for below-grade applications.

- Will not prevent water penetration through structural cracks, defects or open joints.

- May damage glass or be difficult to remove. Always protect.

- Not recommended for horizontal surfaces, including horizontal wood surfaces.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Weather Seal Blok-Guard® & Graffiti Control Ultra 15. Refer to the Product Data Sheet for additional information about application of Blok-Guard® & Graffiti Control Ultra 15. Do not dilute or alter. Stir thoroughly before use. Once opened, Blok-Guard® & Graffiti Control Ultra 15 must be used immediately.

Specifier Note: Lightweight block and extremely porous masonry will need two coats. See “Second Coat Application.”

# Sprayer Application Instructions

- Using low-pressure (less than 50 psi) spray equipment, saturate, “wet-on-wet” from the bottom up. Avoid excessive overlapping.

Specifier Note: when spray applying to fluted architectural block, spray in an “overlapping X pattern” for complete coverage of recessed surfaces.

- Let the first application penetrate the masonry surface for 2 to 3 minutes.

- Immediately brush out runs and drips to prevent build up.

# Brush or Roller Application Instructions

Thoroughly saturate the surface. Avoid excessive overlapping. Brush out runs and drip to prevent buildup.

# Heavily Textured and Porous Surface Application Instructions

Using low-pressure (less than 50 psi) spray equipment, saturate, “wet-on-wet” from the bottom up, applying enough material to create a 6 to 8 inch rundown below the contact point while avoiding excessive overlapping. Let the first application penetrate the masonry surface for 2 to 3 minutes. Reapply in the same saturating manner to ensure complete coverage of recessed surfaces. Immediately brush out runs and rips to prevent build up.

# Dense, Smooth Surface Application Instructions

Apply enough in a single saturating application to completely wet the surface without creating drips, puddles or rundown. Brush out or back roll all runs and drips for uniform appearance. DO NOT OVER APPLY. One application is normally enough.

# Wood Application Instructions

Saturate to the point of rejection. Let first application penetrate 2 to 3 minutes. Reapply in the same saturating manner.

# Second Coat Application Instructions

Apply the second coat as soon as the first coat is dry to touch, or within 2 hours of the first coat. Immediately back roll or brush out runs and drips for a uniform appearance and to prevent build up. Allowing more than 2 hours between coats reduces effectiveness of the second coat.

# Drying Time

Protect treated surfaces from rain for 4 to 6 hours. In normal weather (60 to 80 degrees Fahrenheit [16 to 27 degrees Celsius] at 50 percent humidity), Blok-Guard® & Graffiti Control Ultra 15 dries to the touch in about 25 minutes. Drying takes lower at lower temperatures. Product gains its water-repellency properties in 24 hours.

# Graffiti Removal

Remove most types of graffiti with Defacer Eraser® Graffiti Remover or Enviro Klean® SafStrip.

# Clean-up

Clean tools and equipment immediately with mineral spirits or an equivalent cleaning solvent. Remove over spray and spills as soon as possible.