Sure Klean® Weather Seal Blok-Guard® & Graffiti Control Ultra Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and Safety Data Sheet for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use the manufacturer’s application instructions. Let test area protective treatment cure before inspection. Keep test panels available for comparison throughout the protective treatment project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® Weather Seal Blok-Guard® & Graffiti Control Ultra is a clear, solvent-based silicone elastomer formulated to weatherproof concrete block and other porous masonry materials and protect treated surfaces from repeated graffiti attacks without altering the natural appearance.

Blok-Guard® & Graffiti Control penetrates and fills pores to prevent water penetration through exterior walls exposed to normal weathering. Graffiti removal is fast and easy using Defacer Eraser® Graffiti Remover.

# Typical Technical Data

FORM: Clear liquid, petroleum odor

SPECIFIC GRAVITY: 1.308

pH: not applicable

WEIGHT/GALLON: 10.85 pounds

ACTIVE CONTENT: 9 percent

TOTAL SOLIDS: 9 percent ASTM D 2369

VOC CONTENT: 100 grams per Liter, maximum

FLASH POINT: 100 degrees F (38 degrees C) ASTM D 3278

FREEZE POINT: less than -22 degrees F (less than -30 degrees C)

SHELF LIFE: 1 year in tightly sealed, unopened container

# Limitations

- Not suitable for extremely dense or polished surfaces.

- Not suitable for asphaltic or painted surfaces.

- Not recommended for below-grade applications.

- Will not prevent water penetration through structural cracks, defects or open joints.

- May damage glass or be difficult to remove. Always protect.

- Not recommended for horizontal surfaces, including horizontal wood surfaces.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Weather Seal Blok-Guard® & Graffiti Control Ultra.  Refer to the Product Data Sheet for additional information about application of Blok-Guard® & Graffiti Control Ultra. Do not dilute or alter.

# Vertical Application Instructions

For best results, apply Blok-Guard® & Graffiti Control Ultra “wet-on-wet” to a visibly dry and absorbent surface.

# Spray

- Using low-pressure (<50 psi) spray equipment, saturate, “wet-on-wet” from the bottom up. Avoid excessive overlapping.

- Let the first application penetrate the masonry surface for 2 to 3 minutes. For heavily textured and porous surfaces, reapply in same saturating manner to ensure complete coverage of recessed surfaces.

- Immediately brush out runs and drips to prevent build up.

# Brush or Roller

Thoroughly saturate the surface. Avoid excessive overlapping.  Brush out runs and drip to prevent buildup.

# Fluted Architectural Block

Spray in an "overlapping X pattern" for complete coverage of recessed surfaces.

# Dense, Smooth Surfaces

Apply enough in a single saturating application to completely wet the surface. Avoid excessive overlapping. Back roll all runs and drips for a uniform appearance. One application is normally enough.

# Wood

Saturate to the point of rejection.  Let first application penetrate 2 to 3 minutes. Reapply in the same saturating manner.  Not appropriate for horizontal surfaces.

# Drying Time

Protect treated surfaces from rain for 4 to 6 hours.

# Graffiti Removal

Remove most types of graffiti with Defacer Eraser® Graffiti Remover or Enviro Klean® SafStrip.

# Cleanup

Clean tools and equipment immediately with mineral spirits or an equivalent cleaning solvent. Remove over spray and spills as soon as possible.