Sure Klean® Weather Seal Color Enhancer VOC Specification

Specifier Note: The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s). The Architect should always refer to the Product Data Sheet and Safety Data Sheet for additional recommendations and for safety information.

Specifier Note: Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use the manufacturer’s application instructions. Let test area protective treatment cure before inspection. Keep test panels available for comparison throughout the protective treatment project.

Specifier Note: Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046. Phone: (800) 255-4255; Fax: (785) 830-9797. E-mail: CustomerCare@prosoco.com

# Product Description

Sure Klean® Weather Seal Color Enhancer WB is a solvent-based blend of high-quality siloxanes modified to provide excellent water repellency and color enhancement to interlocking concrete, fired clay, porous tile, and many types of natural stone surfaces.

Color Enhancer VOC penetrates and reacts with the surface to form a chemical bond, providing long-term durability, alkali resistance and superior breathability.

# Typical Technical Data

FORM: clear, colorless liquid; solvent odor

SPECIFIC GRAVITY: 1.06

pH: not applicable

WEIGHT/GALLON: 8.84 pounds

ACTIVE CONTENT: 22 percent

TOTAL SOLIDS: 20 percent ASTM D2369

FLASH POINT: 63 degrees F (17 degrees C) ASTM D3278

FREEZE POINT: 38 degrees F ( 4 degrees C)

SHELF LIFE: 1 year in tightly sealed, unopened container.

VOC CONTENT: 100 grams per Liter

# Limitations

- Not suitable for extremely dense surfaces.

- Over application may result in surface discoloration or sheen.

- Not recommended for below-grade applications.

- Will not prevent water penetration through structural cracks, defects or open joints.

- Always pretest before use around pools or fountains to ensure desired results.

- Not appropriate for application to asphaltic or painted surfaces.

- Not suitable for application to synthetic resin paints, gypsum, plaster or other non-masonry surfaces.

Specifier Note: Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Color Enhancer VOC. Refer to the Product Data Sheet for additional information about application. Apply as packaged. Do not dilute or alter. Mix well before use.

Sprayer Application: Horizontal Surfaces

Apply in a single, saturating application using enough to keep the surface wet for 2 to 3 minutes before penetrating. Lightly broom out puddles. Use clean absorbent towels to pick up excess material that does not immediately penetrate.

Sprayer Application: Vertical Surfaces

Thoroughly saturate the surface using enough for a rundown of 6 to 8 inches below the spray pattern. Brush out heavy runs and drips.

Brush or Roller Application

Saturate the surface. Avoid excessive overlapping. Brush out runs and drips to avoid buildup.

Dense Surface Application

Use a soft cloth or lamb’s wool to apply Color Enhancer VOC. Let it penetrate for 2 to 5 minutes. Wipe up excess.

Second Coat Application

SPECIFIER NOTE: Some highly porous surfaces may need two applications for uniform color enhancement.

Apply the second application when the first coat is dry to touch.

Drying Time: Protect treated surfaces from rain for 4 to 6 hours after application. Protect horizontal surfaces from foot and vehicle traffic for 8 to 12 hours following application. Provide cross-ventilation and fresh air to interior spaces for at least 8 hours following application. Sure Klean® Weather Seal Color Enhancer VOC gains its water repellency properties in 72 hours.

Cleanup: Clean tools and equipment immediately with mineral spirits or an equivalent cleaning solvent. Remove over spray, spills, etc. as soon as possible.