Sure Klean® Weather Seal SL40 <600 Water Repellent Specification

Specifier Note:  The information provided below is intended to guide the Architect in developing specifications for products manufactured by PROSOCO, Inc. and should not be viewed as a complete source of information about the product(s).  The Architect should always refer to the Product Data Sheet and SDS for additional recommendations and for safety information.

Specifier Note:  Paragraph below is for PART 1 GENERAL, Quality Assurance.

# Test Area

Test a minimum 4 ft. by 4 ft. area on each type of masonry. Use the manufacturer’s application instructions. Let test area protective treatment cure before inspection. Keep test panels available for comparison throughout the protective treatment project.

Specifier Note:  Paragraphs below are for PART 2 PRODUCTS, Manufacturers and Products.

# Manufacturer

PROSOCO, Inc., 3741 Greenway Circle, Lawrence, KS 66046.  Phone: (800) 255-4255; Fax: (785) 830-9797.  E-mail:  CustomerCare@prosoco.com

# Product Description

Sure Klean® Weather Seal SL40 <600 is a clear, penetrating silane water repellent. Formulated to comply with US EPA AIM VOC regulations, Sure Klean® Weather Seal SL40 <600 protects concrete and masonry surfaces against intrusion of water and waterborne contaminants. Weather Seal SL40 <600 chemically reacts with the substrate to produce a long-lasting water repellent effect. The product’s low viscosity and small molecular size allows maximum penetration into the concrete or masonry surfaces. Surfaces treated with SL40 <600 maintain their natural appearance, vapor permeability, slip resistance and other surface characteristics.

# Typical Technical Data

FORM: Clear colorless liquid with alcohol odor

SPECIFIC GRAVITY: 0.842

pH: not applicable

WEIGHT PER GALLON: 7.01 pounds

ACTIVE CONTENT: 40 percent

TOTAL SOLIDS: 25 percent ASTM D 5095

FLASH POINT: 35 degrees Fahrenheit (2 degrees Celsius) ASTM D 3278

FREEZE POINT: no data

SHELF LIFE: 1 year in tightly sealed, unopened container

VOC CONTENT: 600 grams per Liter, maximum. Complies with USEPA AIM VOC regulations. Not suitable for sale in states and districts with more restrictive AIM VOC regulations.

# Limitations

- Not appropriate for use on limestone, marble, travertine or other calcareous stones. Always test other natural stone to ensure desired results.

- Not recommended for asphalt or other non-masonry materials.

- Not recommended for below-grade applications or for use under hydrostatic pressure.

- Not suitable for sale in states and districts with more restrictive AIM VOC regulations.

Specifier Note:  Paragraphs below are for PART 3 EXECUTION, Installation.

# Application

Before applying, read “Preparation” and “Safety Information” sections in the Manufacturer’s Product Data Sheet for Weather Seal SL40 <600. Refer to the Product Data Sheet for additional information about application of Weather Seal SL40 <600. Do not dilute or alter. Mix or stir well before use.

Vertical Application Instructions: Apply in a saturating spray application from the bottom up. Apply enough material to produce a 6-inch rundown below the contact point of the spray pattern. For best results on highly porous surfaces, a second saturating application may be required for maximum water repellent effectiveness. Allow 5 to 10 seconds between saturating application.

Horizontal Application Instructions: Apply in a single, saturating application with enough material so treated surfaces stay wet for at least 5 to 10 seconds before penetrating. Any puddles should be broomed thoroughly until they completely penetrate the surface.

# Drying Time

Protect treated surfaces from rain, foot and vehicular traffic for at least 4 hours after application.

# Cleanup

Clean tools and equipment immediately with isopropyl alcohol, denatured alcohol or equivalent cleaning solvent. Remove over spray and spills as soon as possible.